## Slide 1
Production Target developments for the SPES project
Alberto Andrighetto
LNL-INFN
EURSOL Town Meeting - 2012 - Lisbon

## Slide 2
Talk Overview
  The SPES project at LNL.
The production target (TIS).
The target materials for RIB.
The European scenario & perspectives.

## Slide 3
a
b
d
g
The SPES staging
Building + Cyclotron
& ISOL target
N rich RIBs production
& reacceleration
High current RFQ
& neutrons for BNCT
PCyclo & Ncyclo
Protons & neutrons
from cyclotron
Fully Financed
Partially Financed
Partially Financed
The SPES project
Goal: to expand in the future the nuclear physics tests at LNL
SPES is: 1) A second generation ISOL facility (for neutron-rich ion beams)
2) An interdisciplinary research center (for p,n applications)

## Slide 4
Spes (new) building
Exp. Hall 3
ALPI building
Cyclotron
RIB target stations
HRMS
Charge Breeder
RFQ
Expected ground breaking in February 2013
Beam Cooler
SPES project status:

## Slide 5
Target complex – disc & container
Temperature distribution [°C] (ANSYS ®)

## Slide 6
ILine= 200A -> 600A max
ITarget= 700A -> 1200A max
Target & ion source

## Slide 7
The SPES off-line Front end
(working since 2010)
60 kV platform

## Slide 8
The SPES 1+ Ion Sources
SPES SIS
& LIS
SPES PIS

## Slide 9: The isotope release
Release of isotopes from a ISOL target: involved processes
YTarget = Φ ·σ ·N ·εR
f= Injector flux, s = Cross section
N= Target thickness, eR= Release efficiency
The target yield and release efficiency
εR = ediffusion · eeffusion · eionization · etransport
1. In-target reaction (fission)
2. In-target diffusion
3. Effusion from target to ion source
4. Ionization
5. Acceleration and transport
eR takes into account the efficiencies of all the involved processes
Most critical processes for release efficiency, they are affected by:
1) Material composition and density
2) Material microstructural properties
(grain size,porosity, interconnectivity)
3) Working Temperature
(use of high limiting temperature materials)

## Slide 10
Temperature vs yield …
Spes data from HRIBF measurement
T very important for short
lived isotopes!

## Slide 11
First conclusion…
Is necessary to produce for SPES RIB:
Target with high working temperature -> refractory carbides/oxides
2) Material with good characteristics in terms of release (grain and porosity) -> carefully R&D is mandatory!

## Slide 12
Fume hood for wet chemistry with uranium and thorium preparative chemistry.
UNI Padova Radiochemistry Facility
Two dedicated glove boxes for handling and storage of sensitive compounds.
High Vacuum furnace for sample carburization & sintering

## Slide 13
Equipments (1/3)
Mixing and grinding
Glove box for safe operation with actinides
Cold pressing
Manual hydraulic press for f13 mm samples
Hydraulic press for f30 and f40 mm samples
Manual mixing
Mill for automatic mixing

## Slide 14
Equipments (2/3)
Die set
For 13 mm. discs
(Prototype format)
For 40 mm. discs
(SPES format)

## Slide 15
Equipments (3/3)
HT-HV furnace for actinide carbides
HT-HV furnace for other carbides
T up to 2100 °C, P = 10-6 mbar
Horizontal carburization and sintering on a graphite crucible
Treatment of up to 3 f13 mm samples or 1 f40 mm sample
Used for UCX production
T up to 2000 °C, P = 10-6 mbar
Vertical carburization and sintering in a graphite box inside a Ta heater (similar configuration to SPES target)
Treatment of up to 7 f40 mm samples
Used for other carbides production

## Slide 16: Production methods
Carbothermal reaction between the precursor oxide and carbon → commonly used
Direct reaction between metal and graphite → more difficult and expensive
Sol-gel route → a liquid precursor is transformed into a gel that is pyrolized to obtain the carbide at lower T than reaction 1) and 2)
Three different production routes:
MxOy + (2x+y+n)C → xMC2 + yCO + nC (Route 1)
xM + (y+n)C → MxCy + nC (Route 2)
Carbothermal reduction of the precursor oxide (reaction 1) is necessary to operate at high temperature and high vacuum → SPES HT furnace

## Slide 17: Synthesis of carbides
RAW MATERIALS
MIXING AND GRINDING OF THE POWDERS
COLD PRESSING INTO PELLETS
THERMAL TREATMENT
Oxide + carbon source (usually graphite)
Carbothermal reduction of oxides at SPES chemistry laboratories
Manual (mortar) or automatic (planetary mill)
Industrial or home-made dies, up to 90 ton
CHARACTERIZATION OR ON-LINE TESTS
High temperature, high vacuum
Crystal phases, microstructure, thermal properties, porosity evaluation, ecc.

## Slide 18
Among the possible choices for the materials constituting the SPES target, low density, carbon dispersed metal carbides have been chosen.
Actinide carbides
Other refractory carbides
Used for n-rich isotopes production.
High melting point (T > 2000°C)
High limiting temperature
Acceptable thermal conductivity
Good mechanical stability
UCX target
Ex: SiC, ZrC, B4C
High melting point (T > 2000°C)
High hardness
Good thermal conductivity
Chemical inertness up to very high T
Main challenging
Target: n-rich vs. p-rich

## Slide 19
Possible p-rich beams for SPES-α
1 H |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 He
3 Li | 4 Be |  |  |  |  |  |  |  |  |  |  | 5 B | 6 C | 7 N | 8 O | 9 F | 10 Ne
11 Na | 12 Mg |  |  |  |  |  |  |  |  |  |  | 13 Al | 14 Si | 15 P | 16 S | 17 Cl | 18 Ar
19 K | 20 Ca | 21 Sc | 22 Ti | 23 V | 24 Cr | 25 Mn | 26 Fe | 27 Co | 28 Ni | 29 Cu | 30 Zn | 31 Ga | 32 Ge | 33 As | 34 Se | 35 Br | 36 Kr
37 Rb | 38 Sr | 39 Y | 40 Zr | 41 Nb | 42 Mo | 43 Tc | 44 Ru | 45 Rh | 46 Pd | 47 Ag | 48 Cd | 49 In | 50 Sn | 51 Sb | 52 Te | 53 I | 54 Xe
55 Cs | 56 Ba |  | 72 Hf | 73 Ta | 74 W | 75 Re | 76 Os | 77 Ir | 78 Pt | 79 Au | 80 Hg | 81 Tl | 82 Pb | 83 Bi | 84 Po | 85 At | 86 Rn
87 Fr | 88 Ra |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  | 57 La | 58 Ce | 59 Pr | 60 Nd | 61 Pm | 62 Sm | 63 Eu | 64 Gd | 65 Te | 66 Dy | 67 Ho | 68 Er | 69 Tm | 70 Yb | 71 Lu | 
 |  | 89 Ac | 90 Th | 91 Pa | 92 U | 93 Np | 94 Pu | 95 Am | 96 Cm | 97 Bk | 98 Cf | 99 Es | 100 Fm | 101 Md | 102 No | 103 Lr | 
Alkaline - Alkaline earth metals
Halogens
Noble gases
Post-transition elements
Transition metals
Lanthanides

## Slide 20
p-rich production: B4C target
Possible p-rich elements: Be
Long treatment to produce porous B4C samples
f13 and f40 mm samples produced and characterized

## Slide 21
p-rich production: other targets
SiC target
Other targets
Possible p-rich elements: Al
Disks are purchased already made
f40 mm disks ready and currently used for thermal tests on the target-ion source complex
f30 mm disks used for thermal conductivity measurements
A f13 mm prototype already tested at HRIBF → 26Al
Targets: LaCX, ZrC, oxides
Possible p-rich elements: Cs,I,As,Br, Rb,Na,Mg,Si and others
f40 mm disks ready
f30 mm disks used for thermal conductivity measurements
Production of foams (very porous solids)
LaCX target prototype

## Slide 22
Surface Ion source
Laser beam
Laser with SIS
Main fission (p-> 238U) fragments
Plasma Ion source
1
2
H
He
3
4
5
6
7
9
10
Li
Be
B
C
N
O
F
Ne
11
12
13
14
15
16
17
18
Na
Mg
Al
Si
P
S
Cl
Ar
19
20
21
22
23
24
25
26
27
28
29
30
31
32
33
34
35
36
K
Ca
Sc
Ti
V
Cr
Mn
Fe
Co
Ni
Cu
Zn
Ga
Ge
As
Se
Br
Kr
37
38
39
40
41
42
43
44
45
46
47
48
49
50
51
52
53
54
Rb
Sr
Y
Zr
Nb
Mo
Tc
Ru
Rh
Pd
Ag
Cd
In
Sn
Sb
Te
I
Xe
55
56
57
72
73
74
75
76
77
78
79
80
81
82
83
84
85
86
Cs
Ba
La
Hf
Ta
W
Re
Os
Ir
Pt
Au
Hg
Tl
Pb
Bi
Po
At
Rn
87
88
89
104
105
106
107
108
109
110
111
112
Fr
Ra
Ac
Rf
Db
Sg
Bh
Hs
Mt
8
Elements with bad volatility (NOT EXTRACTED)
Surface Ionization Method
Photo Ionization Method
Plasma Ionization Method
Selective method
Very selective method
No selective method
n-rich beams for SPES-β

## Slide 23
n-rich production: UCX targets
1) Standard UCX
Standard carbothermal reduction process using graphite as carbon source
Density is about 4.3 g/cm³
f13 mm target prototype made of 7 disks produced and tested on-line at HRIBF

## Slide 24
n-rich production: UCX targets
2) Low density UCX
Carbothermal reduction process using graphite and carbon nanotubes as carbon source
Density is about 2.6 g/cm³
f13 mm target prototype made of 7 disks produced and tested on-line at HRIBF

## Slide 25
Beam from Tandem Accelerator
Beam Diagnostics
Dipole Magnet
M/DM = 2000
Moving Tape System
and g-ray Detector
Target / Ion Source
HRIBF: On-Line TIS Testing Facility
low intensity (<50 nA) tests of RIB production targets

## Slide 26
Targets tested at three different temperatures: 2000°C, 1800°C and 1600°C
Irradiation by 40 MeV, 50 nA proton beam, ionization with plasma ion source
21 elements, about 75 isotopes collected
Yield vs. half-life characterization
 | Standard UCX | Low density UCX
Density (g/cm³) | 4.25 | 2.59
Diameter (mm) | 12.50 | 13.07
Thickness (g/cm²) | 0.41 | 0.41
Calculated porosity (%) | 58 | 75
Experimental tests at HRIBF
1) Standard UCX

## Slide 27
Yield vs. T1/2
Holdup-time (92Sr)
D. Scarpa et al., Eur. Phys. J. A 47 (2011) 32.
S. Corradetti et al., Eur. Phys. J. A 47 (2011) 119.
1) Standard UCX
Experimental tests at HRIBF

## Slide 28
2) Low density UCX
Targets tested at three different temperatures: 2000°C, 1800°C and 1600°C
Irradiation by 40 MeV, 50 nA proton beam, ionization with plasma ion source
21 elements, about 80 isotopes collected
Yield vs. half-life characterization
 | Standard UCX | Low density UCX
Density (g/cm³) | 4.25 | 2.59
Diameter (mm) | 12.50 | 13.07
Thickness (g/cm²) | 0.41 | 0.41
Calculated porosity (%) | 58 | 75
Experimental tests at HRIBF

## Slide 29
Yield vs. T1/2
New manuscript by S. Corradetti, S. Carturan, M. Manzolaro, D. Scarpa, L. Biasetto, A. Andrighetto, P. Zanonato, P. Colombo, C. Jost and D. W. Stracener in progress
Holdup-time (92Sr)
2) Low density UCX
Experimental tests at HRIBF

## Slide 30
New UCx target
New production 6 g/cm³ (MD) UCX targets
Production process:
1)“Standard” carbothermal reduction synthesis→~4 g/cm³
2) Grinding and re‐pressing of the powders→ to be done
3) Re-sintering of the pellets →to be done
First prototype sample produced with density ~ 6.2 g/cm³

## Slide 31: ISOL FACILITY in EUROPE
LNS -
SPIRAL –
France
CERN
Italy

## Slide 32
The Excyt LNS RIB facility
Target Front End
Target Chamber Unit

## Slide 33: SPIRAL facility at GANIL
(Information from : A.Villari talk)
Stable beams from C to U
0.3A - 1.0A MeV
E =
5A - 13.0A MeV
27A - 95 A MeV
RIB: He, N, O,
F, Ne, Ar, Kr
E < 20A keV
E = 1.7A - 25A MeV
IRRSUD
RIB
E = 25A - 80A MeV
SISSI
3 simultaneous beams at different energies

## Slide 34: ALTO facility at ORSAY
(Information from : C. Lau talk)

## Slide 35: ISOLDE at CERN
Thanks to R. Catherall
Over 100 TIS combinations!

## Slide 36
FP7 ENSAR – the ActiLab JRA
Task 1: Synthesis of new actinide targets (CERN, INFN, IPNO) Subtask 1: Sol-gel synthesis in complex fluids
Subtask 2: Nanostructures
Task 2: Characterization of actinide targets (CERN, INFN)
Subtask 1: Microstructure, porosity, specific surface, crystalline phase
Subtask 2: Emissivity, thermal conductivity at high temperature
Task 3: Actinide targets properties after irradiation (CERN, PSI)
Subtask 1: Post-irradiation examination of target prototypes
Task 4: Online tests of actinide targets (CERN, GANIL, IPNO)
Subtask 1: Impact of pulse time structure on release and ageing properties
Subtask 2: Analysis of the results-effusion and diffusion phenomena

## Slide 37: New UCx target at ISOLDE
(Information from : A. Gotteberg talk)

## Slide 38
IPNO contribution to ActiLab
Thanks to C. Lau
UCX Laboratory:
Extension works completed (April 2012)
New heating bench for fast and programmable carburization is operational (May 2012)
Gas and water supply in the extended UCX Lab (Nov. 2012)
Contribution to ACTILAB:
Carburization and analysis of UO2+CNT pellets from ISOLDE (shipping in progress)
Contribution to woks on HD UC pellets (Rosatom - Russia) tested at ISOLDE
Contribution to next experiment at ISOLDE (IS540)
New heating bench
Extension of the UCX Lab

## Slide 39
IPNO contribution to ActiLab
10 mm
Dense (13.5) and porous (40%), with high level of PFs release at 1550°C
R&D on UCX in progress:
ALTO leads a R&D program on UCX synthesis, exploitation and reprocessing with the collaboration of the radiochemistry and the Chemistry Sciences (Rennes) groups.
Nuclear Instruments and Methods in Physics Research B 288 (2012) 34–41
“An off-line method to characterize the fission product release from
Uranium-carbide-target prototypes developed for SPIRAL2 project ”
Cf. Poster by S. Tusseau-Nenez:
“Uranium-carbide-target prototypes for SPIRAL2 project:
fission product release and physicochemical properties”

## Slide 40
New post-doc position at LNL-INFN in the framework of
‘UCX production, characterization and on-line testing’
Investigated topics:
Influence of starting materials characteristics (powders size, composition, mixing and grinding operation) on the final UCX properties
Goal: test of the produced UCX targets at ALTO facility
for the evaluation of microstructure and release of isotopes
LNL contribution to ActiLab

## Slide 41
UCX developement - ActiLab
INFN – LNL Activity
New radiochemistry laboratory at LNL-INFN, setup on progress.
‘Old’ radiochemistry laboratory at Padova University, after a long period o maintenance, is now fully operative
Acquisition of a micromill and sieves to perform granulometry analysis on the starting and final powders

## Slide 42
Decontamination room
LNL new Radiochemistry Facility
Devices: glove box , fume hood , high vacuum furnace
UCx Laboratory (working in progress…)
Estimated end of works: Dec ‘12

## Slide 43
Thanks for your attention!
The SPES-TIS group